MTR Verification Checklist

Quick Reference Card · FreeDocumentsHub.com

Required Fields on a Genuine MTR

- Heat / Lot / Cast Number — matches the physical marking on the material

- Material Specification & Grade (e.g., ASTM A106 Gr. B)

- Mill / Manufacturer Name & Location

- Chemical Composition (C, Mn, P, S, Si, Cr, Ni, Mo, etc.)

- Mechanical Properties (yield, tensile, elongation, hardness, impact values)

- Heat Treatment Condition

- Dimensions / Size / Quantity matching the PO

- NDT Results (where applicable)

- EN 10204 Certificate Type (2.1 / 2.2 / 3.1 / 3.2)

- Mill Stamp, Certificate Number & Authorized Signature

EN 10204 Certificate Types At a Glance

| Type | Independent Check? | Typical Use |
| --- | --- | --- |
| 2.1 | No | Declaration of compliance — general, non-critical material |
| 2.2 | No | Test report from non-specific (batch) inspection |
| 3.1 | Internal, independent dept. | Standard requirement — ASME / Aramco pressure equipment |
| 3.2 | External / third-party | Highest assurance — critical service, AI witness required |

Red Flags — Stop and Verify Before Accepting

- No heat/lot number, or it doesn't match the material marking

- 'Perfect' or identical values across unrelated certificates

- Missing mill letterhead, logo, or contact details

- No signature, stamp, or certificate number

- Mill name cannot be independently verified

- Low-resolution scan with visible editing artifacts

- Certificate type doesn't match the project specification

Need help building an audit-ready documentation package? Visit FreeDocumentsHub.com — Saudi Aramco AVL & ASME vendor documentation services