WELDING PROCEDURE SPECIFICATION (WPS)

Sample Format — As per ASME Section IX

| DOCUMENT CONTROL |  |  |  |
| --- | --- | --- | --- |
| WPS No. | FDH-WPS-001 | Rev. No. / Date | 0 / 30-Jun-2026 |
| Supporting PQR No. | FDH-PQR-001 | Code & Edition | ASME Section IX, 2023 |
| Welding Process(es) | GTAW + SMAW | Type | Manual |

| JOINTS (QW-402) |  |  |  |
| --- | --- | --- | --- |
| Joint Type | Butt Joint, Single V-Groove | Backing | With Backing — Consumable Insert |
| Root Opening | 1.6 mm ± 0.8 mm | Root Face | 1.6 mm ± 0.8 mm |
| Groove Angle | 60° ± 5° | Backing Material | Same P-No. as Base Metal |

| BASE METALS (QW-403) |  |  |  |
| --- | --- | --- | --- |
| Material Spec. | ASTM A106 Gr. B | P-No. / Group No. | P-1 / Gr. 1 |
| To Material Spec. | ASTM A106 Gr. B | To P-No. / Group No. | P-1 / Gr. 1 |
| Thickness Range Qualified | 5 mm to 40 mm | Diameter Range Qualified | All Diameters (≥ 73 mm) |

| FILLER METALS (QW-404) |  |  |  |
| --- | --- | --- | --- |
| AWS Classification | ER70S-2 (Root) / E7018 (Fill/Cap) | F-No. | F-6 / F-4 |
| A-No. | A-1 | Filler Metal Size | 2.4 mm (Root) / 3.2 mm (Fill/Cap) |
| Flux / Consumable Insert | N/A (Solid Wire / Covered Electrode) | Filler Metal Product Form | Solid Wire / Covered Electrode |

| POSITION (QW-405) |  |  |  |
| --- | --- | --- | --- |
| Position(s) of Groove | 6G | Welding Progression | Uphill |

| PREHEAT (QW-406) |  |  |  |
| --- | --- | --- | --- |
| Minimum Preheat Temp. | 10°C (Ambient, min.) | Maximum Interpass Temp. | 250°C |
| Preheat Maintenance | As required between passes | Preheat Method | Gas Torch / Electric Resistance |

| POST-WELD HEAT TREATMENT (QW-407) |  |  |  |
| --- | --- | --- | --- |
| PWHT Required | Yes — Thickness ≥ 19 mm | Temperature Range | 595°C to 635°C |
| Holding Time | 1 hr per 25 mm (min. 30 min) | Heating / Cooling Rate | ≤ 220°C/hr above 425°C |

| GAS (QW-408) |  |  |  |
| --- | --- | --- | --- |
| Shielding Gas | 100% Argon | Flow Rate | 8 – 12 LPM |
| Backing / Purge Gas | 100% Argon | Purge Flow Rate | 5 – 8 LPM |

ELECTRICAL CHARACTERISTICS & WELDING TECHNIQUE (QW-409 / QW-410)

| Pass | Process | Filler Dia. (mm) | Current / Polarity | Amps (A) | Volts (V) | Travel Speed (mm/min) |
| --- | --- | --- | --- | --- | --- | --- |
| Root | GTAW | 2.4 | DCEN | 80 – 110 | 10 – 14 | 50 – 90 |
| Hot Pass | SMAW | 3.2 | DCEP | 90 – 130 | 21 – 26 | 100 – 150 |
| Fill | SMAW | 3.2 | DCEP | 100 – 140 | 22 – 27 | 100 – 150 |
| Cap | SMAW | 3.2 | DCEP | 95 – 135 | 22 – 26 | 90 – 140 |

| Heat Input (Max.) | 1.5 kJ/mm | Technique | Stringer Bead |
| --- | --- | --- | --- |
| String / Weave Bead | Stringer (Root) / Slight Weave (Fill-Cap) | Multi-pass / Single Pass | Multi-pass, Multi-electrode: No |
| Cleaning / Interpass Cleaning | Wire Brush / Grinding | Peening | Not Permitted |

| APPROVAL |  |  |
| --- | --- | --- |
| Prepared By | Reviewed By | Approved By |
| ______________________ Welding Engineer Date: ____________ | ______________________ QA / QC Manager Date: ____________ | ______________________ Project Manager / Client Rep. Date: ____________ |

This is a sample WPS format for reference and training purposes only, provided free by FreeDocumentsHub.com. Values shown are illustrative and must be verified and qualified against an actual Procedure Qualification Record (PQR) before use on any production weld. For project-ready, fully formatted WPS and WQR document packs, visit www.freedocumentshub.com.