PQR ↔ WPS QUICK REFERENCE

ASME Section IX — Procedure Qualification Record Essentials

| What a PQR Must Record (Actual, As-Run Values) - Welding process(es) used - Base metal P-No. / Group No. - Filler metal F-No. / A-No. - Test coupon & deposited weld metal thickness - Preheat / interpass temperature - PWHT time & temperature (if performed) - Shielding / backing gas - Test coupon welding position Test Results That Must Be Attached - Tensile test results - Guided bend test results - Impact test results (if toughness required) - Hardness test results (if required) | The Chain of Custody - 1. Weld witnessed test coupon - 2. Record actual variables as-run - 3. Send coupon for mechanical / NDE testing - 4. Document pass results on the PQR - 5. PQR supports WPS production range - 6. Welder qualified within WPS range - 7. Production weld traceable to all of the above Top PQR-to-WPS Non-Conformances - WPS range wider than PQR data supports - Supplementary essential variables omitted - Deposited thickness misapplied vs. QW-451 / QW-403.6 / QW-403.9 - Production parameters not traceable to any qualified PQR |
| --- | --- |

| Document | Form | What It Proves |
| --- | --- | --- |
| PQR | QW-483 | A specific variable set produced a code-compliant weld |
| WPS | QW-482 | The production-acceptable range those PQR(s) support |
| WPQ | QW-484 / QW-485 | An individual welder can weld within a qualified range |

Need Your Package Reviewed Before an Audit? reviews and builds WPS/PQR packages for Aramco AVL and ASME compliance. WhatsApp: +966-XX-XXX-XXXX