SAMPLE — Procedure Qualification Record (PQR)

Illustrative example based on ASME Section IX suggested format QW-483 — Supports WPS-SMAW-CS-01

Before You Use This This is a filled sample for training and reference only. It illustrates how a PQR should be structured and populated — it is NOT a substitute for an actual witnessed qualification test. A real PQR must record only actual, as-run values from a coupon your organization welded and tested, with laboratory reports attached and signed by an authorized representative.

| Company / Organization Name |  |
| --- | --- |
| Organization Sample Fabrication Works LLC | PQR No. / Date PQR-SMAW-CS-01 / 15-Jun-2026 |
| WPS No.(s) Supported WPS-SMAW-CS-01 | Welding Process(es) / Type SMAW / Manual |
| Joints (QW-402) — Actual |  |
| Joint Design (as welded) Single V-groove, 60° included angle, 3 mm root gap, open root | Backing None — back-gouged and back-welded |
| Base Metals (QW-403) — Actual |  |
| P-No. / Group No. P-No. 1, Gr. 1 to P-No. 1, Gr. 1 | Specification and Type/Grade ASTM A516 Gr. 70 to ASTM A516 Gr. 70 |
| Test Coupon Thickness 3/4 in (19 mm) | Diameter (if pipe) N/A — plate coupon |
| Filler Metals (QW-404) — Actual |  |
| Spec. No. (SFA) / AWS Classification SFA-5.1 / E7018 | F-No. / A-No. F-No. 4 / A-No. 1 |
| Filler Metal Size(s) Used 3/32 in (2.4 mm) root; 1/8 in (3.2 mm) fill/cap | Weld Metal Deposit Thickness (as-run) 19 mm (coupon as-welded thickness) |
| Position (QW-405) — Actual |  |
| Position of Test Coupon 1G (Flat, rolled) | Welding Progression Uphill |
| Preheat (QW-406) — Actual |  |
| Preheat Temperature (as-run) 60°F (15°C) | Interpass Temperature (as-run, max recorded) 410°F (210°C) |
| Postweld Heat Treatment (QW-407) — Actual |  |
| Temperature (as-run) 1,150°F (621°C) | Time (as-run) 1 hour |
| Gas (QW-408) — Actual |  |
| Shielding Gas / Flow Rate N/A (SMAW) | Backing Gas None |
| Electrical Characteristics (QW-409) — Actual |  |
| Current / Polarity (as-run) DCEP | Amperage / Voltage (as-run, recorded range) 105–130 A / 22–25 V |
| Technique (QW-410) — Actual |  |
| Travel Speed (as-run) 5.2 in/min (132 mm/min) average | String or Weave / Passes String bead, multipass, 9 passes |

Tensile Test Results (QW-150)

| Specimen | Width (in) | Thickness (in) | Area (in²) | Ultimate Load (lb) | Tensile Strength (psi) | Failure Location |
| --- | --- | --- | --- | --- | --- | --- |
| T-1 | 0.752 | 0.748 | 0.5625 | 39,400 | 70,044 | Base metal |
| T-2 | 0.750 | 0.750 | 0.5625 | 39,100 | 69,511 | Base metal |

Guided Bend Test Results (QW-160)

| Specimen | Type | Result |
| --- | --- | --- |
| B-1 | Side Bend | No cracks or open defects exceeding 1/8 in — Acceptable |
| B-2 | Side Bend | No cracks or open defects exceeding 1/8 in — Acceptable |
| B-3 | Side Bend | No cracks or open defects exceeding 1/8 in — Acceptable |
| B-4 | Side Bend | No cracks or open defects exceeding 1/8 in — Acceptable |

Certification: We certify that the statements in this record are correct and that the test coupon was prepared, welded, and tested in accordance with the requirements of ASME Section IX.

| Manufacturer Sample Fabrication Works LLC | Date 15-Jun-2026 |
| --- | --- |
| Certified By ________________________ (Authorized Representative) | Title Welding Engineer / QC Manager |

Need Your Own PQR Witnessed, Tested, and Documented? Shammari Smart Systems coordinates witnessed qualification testing and prepares audit-ready WPS/PQR packages for Aramco AVL and ASME code compliance. WhatsApp: +966-XX-XXX-XXXX (update with live number).