SAMPLE — Welding Procedure Specification (WPS)

Illustrative example based on ASME Section IX suggested format QW-482 — SMAW, Carbon Steel Plate

Before You Use This This is a filled sample for training and reference only. It illustrates how a WPS should be structured and populated — it is NOT a qualified procedure and must not be used for production welding as-is. Every WPS you put into production must be supported by your own Procedure Qualification Record (PQR), qualified under your organization's welding program per ASME Section IX.

| Company / Organization Name | WPS No. & Supporting PQR No. |
| --- | --- |
| Organization Sample Fabrication Works LLC | WPS No. / Rev. WPS-SMAW-CS-01 / Rev. 0 |
| Supporting PQR No.(s) PQR-SMAW-CS-01 | Date / Authorized By 07-Jul-2026 / Chief Welding Engineer |
| Welding Process(es) Shielded Metal Arc Welding (SMAW) | Type Manual |
| Joints (QW-402) |  |
| Joint Design Single V-groove, 60° included angle, 1/8 in (3 mm) root gap, 1/16 in (1.5 mm) root face | Backing None (open root, backgouged and back-welded) |
| Base Metals (QW-403) |  |
| P-No. / Group No. (to P-No. / Group No.) P-No. 1, Gr. 1 to P-No. 1, Gr. 1 | Specification and Type/Grade ASTM A516 Gr. 70 to ASTM A516 Gr. 70 |
| Base Metal Thickness Range — Groove 1/8 in (3 mm) to 1-1/2 in (38 mm) | Base Metal Thickness Range — Fillet All thicknesses |
| Filler Metals (QW-404) |  |
| Spec. No. (SFA) / AWS Classification SFA-5.1 / E7018 | F-No. / A-No. F-No. 4 / A-No. 1 |
| Size(s) of Filler Metal 3/32 in (2.4 mm) root; 1/8 in (3.2 mm) fill and cap | Weld Metal Deposit Thickness Range Up to 1-1/2 in (38 mm) [1.1 × coupon thickness] |
| Position (QW-405) |  |
| Position(s) of Groove 1G, 2G, 3G, 4G (All positions qualified) | Welding Progression Uphill |
| Preheat (QW-406) |  |
| Preheat Temp., Minimum 50°F (10°C) | Interpass Temp., Maximum 450°F (232°C) |
| Postweld Heat Treatment (QW-407) |  |
| Temperature Range 1,100–1,200°F (593–649°C) | Time Range 1 hour per inch of thickness, 1 hour minimum |
| Gas (QW-408) |  |
| Shielding Gas / Flow Rate N/A (SMAW — flux-shielded) | Backing Gas None |
| Electrical Characteristics (QW-409) |  |
| Current / Polarity DCEP (Direct Current Electrode Positive) | Amperage / Voltage Range 90–140 A / 21–26 V |
| Technique (QW-410) |  |
| Travel Speed Range 4–7 in/min (100–180 mm/min) | String or Weave Bead String bead, max weave width 3× electrode diameter |
| Multipass or Single Pass (per side) Multipass | Peening / Other None |

Need a WPS Built and Qualified for Your Actual Process? Shammari Smart Systems prepares and qualifies WPS/PQR packages for fabricators and workshops pursuing ASME code compliance and Aramco AVL registration. WhatsApp: +966-XX-XXX-XXXX (update with live number).