NDT Methods Quick Reference Chart

All 10 Non-Destructive Testing Methods — Companion to the FreeDocumentsHub NDT Crash Course

| Method | Acronym | Finds | Surface/Volumetric | Materials | Key Standard | Typical Use |
| --- | --- | --- | --- | --- | --- | --- |
| Visual Testing | VT | Surface flaws, fit-up, profile, dimensions | Surface | All materials | ASME V Art. 9 | Every joint, first-line inspection |
| Liquid Penetrant | PT | Surface-breaking cracks & porosity | Surface | Non-magnetic metals, ceramics | ASME V Art. 6 | Stainless steel & aluminum welds |
| Magnetic Particle | MT | Surface & near-surface cracks | Surface/Near-surface | Ferromagnetic metals only | ASME V Art. 7 | Carbon steel welds, forgings, castings |
| Radiographic | RT | Internal voids, porosity, inclusions | Volumetric | Most metals | ASME V Art. 2 | Critical butt welds, permanent record |
| Ultrasonic (conventional) | UT | Internal cracks, laminations, thickness | Volumetric | Most metals, plastics | ASME V Art. 4/5 | Field crack detection, thickness survey |
| Phased Array UT | PAUT | Internal flaws, precise sizing & mapping | Volumetric | Most metals | ASME V Art. 4 App. I | Critical girth welds, digital audit trail |
| Time-of-Flight Diffraction | TOFD | Through-wall crack height sizing | Volumetric | Most metals | ASME V Art. 4 App. III | Fitness-for-service, sizing with PAUT |
| Eddy Current | ET | Surface cracks, conductivity, coatings | Surface/Near-surface | Conductive materials | ASME V Art. 8/26 | Heat exchanger & condenser tubing |
| Acoustic Emission | AE | Active/growing defects under load | Volumetric (global) | Vessels, tanks, pipelines | ASME V Art. 12 | Proof testing, in-service monitoring |
| Leak Testing | LT | Through-wall leaks, seal integrity | Volumetric | Sealed vessels & piping | ASME V Art. 10 | Final pre-commissioning acceptance |

Notation: H = Hold Point   W = Witness Point   R = Review-only, per your project ITP.

FreeDocumentsHub.com — WPS, PQR, ITP, MTR & MDR documentation for Aramco AVL, ASME, and oil & gas vendor registration. WhatsApp ordering, 24/7.